## BOARD OF TECHNICAL EDUCATION

PORVORIM-GOA

April, 2013 Examinations

Programme: Mechanical Engg./P

Subject: Tool Engineering-II[Press Tools](5077)

# Time Duration: 3 Hrs.                                               Max. Marks:  75

Instructions: 1) All Questions are compulsory.

2) Figures to the right indicate full marks.

3) Assume suitable additional data if required.

| Q.No.1. | Design and draw a die to produce sheet metal component as shown in Fig.‘A’. The component is made of Aluminium having an ultimate shear strength of 275N/mm2. Your design should include: | (50) |
| --- | --- | --- |
|  | - At least two views of the die - Economic strip layout - Bill of materials - Press tonnage calculations. |  |
| Q.No.2. | Answer any two of the following Questions: | 2 x 5 = 10 |
| a) | Explain the ‘U’ Bending process. |  |
| b) | List the variables that affect metal flow during drawing. |  |
| c) | Calculate the blank diameter to draw a cup of 100mm  having a height of 40mm and thickness of 2mm. |  |
| Q.No.3. | Write short notes on any three: | 3 x 5 = 15 |
| a) | Bend allowance |  |
| b) | Piercing operation |  |
| c) | Strech forming |  |
| d) | Embossing and coining dies |  |
| e) | Deep drawing |  |