## BOARD OF TECHNICAL EDUCATION

PORVORIM-GOA

November, 2014 Examinations

Programme: Fabrication Technology & Erection Engg.

Subject: Materials & Processes(4238)

# Time Duration: 3 Hrs.                                               Max. Marks:  75

Instructions: 1) All Questions are compulsory.

2) Figures to the right indicate full marks.

3) Assume suitable additional data if required.

| Q.No.1. | Answer any five of the following Questions: | 5 x 3 = 15 |
| --- | --- | --- |
| a) | Explain centerline cracking of weld. |  |
| b) | Give 3 applications of Ferritic stainless steel. |  |
| c) | Comment upon Timber as an Engineering material. |  |
| d) | What is BOS and BOF in manufacture of steel? |  |
| e) | What is the effect of carbon percentage on melting of plain carbon steel? |  |
| f) | What is alloy cast iron? What are the applications of this alloy? |  |
| g) | How will you use spark test for steel identification? |  |
| h) | What is stress relieving of metal? |  |
| Q.No.2. | Answer any two of the following Questions: | 2 x 6 = 12 |
| a) | Explain the meaning of , , ,  structure of plain carbon steel. |  |
| b) | What is the effect of presence of following elements in steel: i) Silicon ii) Manganese iii) Sulphur iv) Phosphorus. |  |
| c) | Write notes on: i) Tool steels ii) Heat Resistance steel. |  |
| Q.No.3. | Answer any two of the following Questions: | 2 x 6 = 12 |
| a) | Give classification of cast Iron. What are the applications of F.G. Iron and S.G Iron? (Mention 3 applications each) |  |
| b) | Discuss the Mild steel tensile test behaviour and results of the same. |  |
| c) | Which gases play a role in welding and how do they affect the properties of weld? |  |
| Q.No.4. | Write notes on any two: | 2 x 6 = 12 |
| a) | Weld cracking and types of cracks formed |  |
| b) | Corrosion of welds |  |
| c) | Any two methods of reducing welding stresses |  |
| Q.No.5. | Answer any two of the following Questions: | 2 x 6 = 12 |
| a) | Draw a sketch and explain the cold rolling process. |  |
| b) | Is work hardening beneficial to industry? Give applications of this process. |  |
| c) | Describe the process of Age-hardening of Al-Zn system. |  |
| Q.No.6. | Write short notes on any three: | 3 x 4 = 12 |
| a) | Commonly used alloying elements in Alloy steel |  |
| b) | Weight and colour as means of identifying metals |  |
| c) | Salt bath process of heat treatment of steel |  |
| d) | Normalising - effects method and reasons |  |
| e) | Glass and its industrial uses |  |

***********